全介质自承式（ADSS）光缆技术参数表

All Dielectric Self-Supporting Optical Cable (ADSS) Technical Parameters

200米跨距AT/PE护套料110Kv以上(8芯---24芯)

200M span AT/PE sheath above 110Kv(8fibers-24fibers)

ADSS-24B1      光缆外径φ12.4mm

ADSS-24B1       Cable O.D.:12.4mm

| 结构参数 structural parameters | 中心加强件 FRP Central Strength Member FRP | 直径 2.1 mm Diameter:2.1mm |
| --- | --- | --- |
|  | 松套管（填充纤膏） Loose tube(filling gel) | 外径 2.0 mm O.D.;2.0mm |
|  | 内套管 Inner sheath | 厚度 0.9 mm Thickness:0.9mm |
|  | 机械加强层 芳纶 Mechnicall strength：Aramid yarns | 面积 14 mm2 size: mm2 |
|  | 外护套 Outer sheath | 厚度 1.70 mm Thickness:1.70mm |

| 技术参数 Technical Parameters | 光缆外径 O.D.: | 12.4 mm |
| --- | --- | --- |
|  | 光缆截面积 Cable sectional area | 121 mm2 |
|  | 光纤型号 Fiber type | G.652 |
|  | 光缆重量 Cable weight | 134 kg/km |
|  | 额定抗拉强度(RTS) Max.tensile strength | 17.5 kn |
|  | 最大允许使用张力 MAT) Max. allowed of tension | 6.9 kn |
|  | 年平均运行张力 (EDS) Average annual operation tension | 4.36 kn |
|  | 杨氏摸量 Young modulus | 14.1 kn/mm2 |
|  | 热膨胀系数 cocoefficient of thermal expansion thermal expansivity | 4.4 10-6/℃ |
|  | 抗压强度 compression strength | 长期 1100 n/100mm Long term |
|  |  | 短期 2200 n/100mm Short term |
|  | 最小弯曲半径 Min.Bending Radius | 运行 220 mm Opperation |
|  |  | 敷设 360 mm Installation |
|  | 适用温度范围 Available temperature | 敷设 -15∽ +60℃ Installation |
|  |  | 运输和运行-40∽ +70℃ Operation |
|  | 光纤余长 Fiber long more than | 0.5∽0.7% |
|  | 外护套类型 Outer sheath type | 耐电痕AT护套料/PE护套料 AT/PE Sheath |
|  | 抗电腐蚀措施 Resistance to corrosion measures | 光缆外护套采用北欧化工耐电痕护套料6081，具有良好的抗电腐蚀性 The fiber optic cable sheath used Nordic chemical resistance to electricity mark covering materials for 6081, has good corrosion resistance to electricity |
| 注:覆冰5MM ice coating |  |  |